MODE I CRACK – REMOTE LOADING

- Tractions at infinity

- Infinite crack  :

- Infinite medium

- Case of plane strain

- Stresses in terms of polar coordinates (Exact Solution)

Solution = stress field approximation in a finite crack around the tip in the origin

- Stresses in terms cartesian coordinates

Application of Gradient Model       ;

Target: Non-Singular Stress Estimation near the crack tip

Boundary Conditions:

- far field coincidence of stresses:

- annihilation of stresses at the origin:

- No tractions on crack surfaces:    ;      [i.e.  ,  , ]

REMARKS

  - The solution is exact for the infinite crack

  - As in classic elasticity it could be used for the stress field description near the tip of the finite crack

CARTESIAN STRESS COMPONENTS FORMULAS & PLOTS

Classical Stress singular	Gradient Stress non-singular

Classical Stress singular	Gradient Stress non-singular

Classical Stress singular	Gradient Stress non-singular

Classical Stress singular	Gradient Stress non-singular

APPENDIX

# Text boxes

x

y

Crack Surfaces:

unloaded

y

x

0